## Slide 1
OER Catalysts for Acidic Media
PEM Electrolyzer
Low pH environment (pH ~0-2)
Poor stability of many catalyst materials
Historically, only Ru and Ir-based catalysts have exhibited acid-stability
Major need to explore non-noble metal acid stable catalysts that exhibit high catalytic activity
High Cost
Low availability
Kibsgaard, J., et. al. Nat Energy 2019.

## Slide 2
OER Catalysts for Acid-Stable Systems – Gen 1 MAP
Acid stable OER catalyst design by treating activity and stability as decoupled elements of catalyst design
Eg: Co Mn Ox (Huynh et. al. Chem. Sci. 2017.)
Structural Element
Active Metal Center
MnOx
CoOx
CoMnOx
Exploration of various active & structural mixed metal oxides (M = 1-4)
Synthesis via electrodeposition for large parameter space
Reduced Metal Oxides
Metal Alloy Systems
Substrate Effects
Ion Insertion
Future Gen

## Slide 3
Measurement Parameters – Electrochemical Module
Cyclic Voltammetry
EIS
Linear Sweep Voltammetry
Chronoamperometry
Overpotential (ƞ)
Reaction kinetics
ECSA
Lifetime stability
Charge-transfer resistance
Faradaic efficiency
Gas Analyzer
O2 Reduction (Pt electrode)
On-Board Electrochemistry
Performance Descriptors

## Slide 4
Measurement Parameters – Characterization Module
LIBs
XRF
Elemental
Composition
SAXS
Imaging (Optical/Electron)
Profilometry
QC Balance
Multi-Gas analysis
Calcination
ICP
Scanning Probe E-Chem
Spectroscopy (FTIR etc.)
Elemental Composition
Performance Descriptors
Future Considerations/Expansions
Adapt for Other E-Chem Systems

## Slide 5
E-MAP – Conceptual Station Progression
Robot
Solution
Module
Electrochemical
Module
Characterization
Module
Calcination
Module
“360⁰” Movement
Ability to program movement across multiple station “visits”
Single robot access to every platform
<
<
Future Gen

## Slide 6
Concept Images – 3D Render (In progress)
Not Pictured: E-Chem Module, under design
Not Pictured: Char. Module – “Probe” on board, rest off of platform
Echem
Char
Soln Handling

## Slide 7
Liquid Handling (x3)
(Need More?)
2. Solid Dispenser Carousel
(To be Updated?)
3. Gripper + Weigh Scale
4, Slide Hotel (FTO slides)
5. Pipette Station
6. Mixing Plate? (not shown)
Modular solution preparation platform that can easily be modified to support various solid/liquid
mixing protocols
Tecan XC Syringe Pump
Combined gripper + weigh scale
1
2
3
4
5
6
Solution Module – Current Inventory

## Slide 8
Solution Module – Example Experiment (Ternary Addition)
Salt (cation/anion)
Concentration
Deposition Additives
Precursor Order
Solution Preparation
Gen 1

## Slide 9
Solution Module – Input/Outputs + Sizes
Inputs:
Mass/volume salt (precursor sol’n)
Mass/volume solvent
Outputs:
Deposition Solution
Standard Sizes:
Mixing Vial – Accom. 5 mL
(5 mL will be total mix volume target)
Stock solutions of precursors will be on-board
Target addition range ~100 µL of each
Solvent addition up to 5 mL
If solid addition, range will be in ng - µg range

## Slide 10
From benchtop to automated platform
  3 electrode cell configuration
  Retrieval of WE (FTO slide) for analysis
  Electrolyte addition/removal
  On-board probe washing
  Miniaturization of electrochemical components
  Multi-cell scale-up
Concept Drawing
Electrochemistry (Echem) Module – 2x Cells
Benchtop

## Slide 11
Cell Design
Inspiration from the redox.me bottom-loaded cell
Flexibility while also being able to more easily incorporate robotics/automation
Reconstructed to fit a smaller design space, less electrolyte volume (5 mL total)
https://redox.me/
NRC / North Design

## Slide 12
Cell Design – Measurement “Probes” - Outputs
1a
2
3
Potentiostat Connections
1a. Connection to loaded glass slide (outside of wall)
1b. Loaded glass slide
2. Reference Electrode
3. Counter Electrode
1b
O2 Analyzer
4. Spectral Probe (will require testing and development)
4
Camera
5. Through camera?
5
(MAYBE) Agitation/Propeller?
6. Something to stir solution (bubble remover)
6
Solid Block

## Slide 13
Cell Design – Liquid In/Out + Washing
1
Liquid In/Out
1a. Loading Tube to draw liquid in/out
1b. Some type of pipette system
Solid Block
2
Spray (Wash) Nozzle
2. DI water spray to wash probes

## Slide 14
Washing the cell stations
Purpose is to wash prior to each new trial run, as new electrolyte will be used for each run
1. Bath Wash
Fill separate vial with water and place onto lid set-up
Will require subsequent washing steps, likely some solvent change, possibly
some motion (rotation?) to help “stir” solution?
A simple dip may be sufficient enough…checking experimentally
2. Spray Wash
Use a nozzle to lightly spray the electrolyte off of the 3 electrodes
Should be gentle “running” over the electrodes
Can build into the lid?
Spray nozzle
on side?
Spray nozzle
built into lid?

## Slide 15
EChem Module – Input/Output – Deposition Cell
Inputs (Software):
Potentiostat
Electrochemical Profile
Programmed current/voltage profile
Inputs (Physical):
Glass Slide
Deposition Solution
Outputs (Physical):
Glass slide w/ catalyst deposition

## Slide 16
EChem Module – Input/Output – Characterization Cell
Inputs (Software):
Potentiostat
Electrochemical Profile
Programmed current/voltage profile
Inputs (Physical):
Coated Glass Slide
Characterization Solution
Outputs (Software):
Potentiostat
Electrochemical
Current/Voltage Response
Performance Descriptors
O2 Analyzer (Char Cell Only)
O2 Evolution profile
Camera
Image

## Slide 17
EChem Module – Sizing & Components
Glass Slide
25 mm x 25 mm x 2.2 mm
Cell Body
Accommodate at least 5 mL of electrolyte
Still in development
Deposition Cell
Area = 1.5 cm2
No O2 Analyzer
No Agitation
Characterization Cell
Area = 1 cm2
>

## Slide 18
EChem Module Step 1 – ElectroDeposition

## Slide 19
EChem Module Step 2 – ElectroCharacterization

## Slide 20
Elemental Characterization – Characterization Module
High throughput elemental characterization technique used widely in the mining, thin film, and precious metal industry
NRC hosts world leading researcher in this technique (Dr. Mohamad Sabsabi) to design and provide custom polyvalent system
Custom designed to be utilized in-line with MAPs platform
Zhang et. al. 1095, 25, , p. 14-19, 2020.
Laser Induced Breakdown Spectroscopy (LIBS)

## Slide 21
Elemental Characterization Step
Glass Slide
LIBS Front End

## Slide 22
Throughput
Typical Experimental Throughput – Assume Single Cell
  1. Initial guess of composition
  2. Solution mixing – 2 minutes
  3. Electrodeposition – 5 minutes maximum
  4. Electrochemical characterization – 5 minutes (+)
  5. Elemental Analysis – 5-10 seconds
  6. A.I - Data (elemental concentration, potential, current) feed into ChemOS, next target is given
  – 5 minutes
Total ~15 minutes per run
Macleod et. al. arXiv: 1906.05398

## Slide 23: Development Road Map – Solution Module
Confirm workflow and specifications
Simulate workflow of components?
(when?) Begin construction of solution module at NRCan
Further inventory integration

## Slide 24: Development Road Map – EChem Module
Physical Platform
Confirm input/output for platform (various probes etc.)
Model cell design + actuator system (Co-op student?)
Simulate integration into platform
Physical construction of Echem Module
Physical Integration into platform
Instrument Integration
Python wrapper for Biologic SP-150 (VSP-300) (critical!)
O2 sensor integration (Neofox) – Arduino RS-232 Communication (+ others)
Camera module
Software
Workflow and Operations (all equipment)

## Slide 25: Development Road Map – Characterization Module
Physical Platform
Design of loading platform for LIBS probe
Workflow for platform loading
Software
How to proceed with in-house developed integration?
Integration onto platform

## Slide 26
(Condensed) Example Work Flow
Addition
Transfer
Solution Module
EChem module
EChem module
Char Module

## Slide 27
Project Timeline
Physical Platform
Initial Construction (Solution Platform) – May 2020
Echem Module Design and Development – May 2020 – Sept. 2020
Initial Automated Capabilities & Further Platform Development – Oct. 2020 – June 2021
Iterative Design, Expansions, and Coupling to AI & Database – Oct. 2020 – Jan 2022
Machine Learning/AI
Parallel Project under MCF Challenge Program – May 2020 – Apr. 2022
Database & Network Evaluation
Collaborative Project involving other MCF projects, KITs, and NRCan Collaborators – Start May 2020

## Slide 28
Concept Images

## Slide 29
Extra Slides

## Slide 30: R&D Focus – NRC Mississauga
Core Competencies
High Throughput & Closed loop Synthesis (Intelligent Throughput) and Characterization Tools
Computational Material Discovery (Simulation & AI)
Optimization/Performance prediction
Self-Driving Laboratory
Materials and Process Database
Collaborative & AI/ML accessible
Integrate other data from outside sources
MAPs at NRC-M
Engage with other RCs and collaborators to establish
MAPs for accelerated materials discovery in targeted
domains (material or process) of RCs at NRC-M
Database
Notes:     High-throughput experimentation (HTE) (Leader)
NRC-M will collaboratively engage with other RCs and external partners in the design, development, and integration of HTE towards the development of MAPs (robotic, rapid and automated). This also involves development of methods to “scale” representative manufacturing processes for integration into MAPs.
    Computational (AI-driven) materials discovery, design and process simulation (Leader / Collaborator)
This competency will involve establishment and deployment of artificial intelligence / machine learning (AI/ML) and modeling tools that accelerate materials discovery, process scale-up and optimization and predict performance and durability. It will aim to address all critical factors for successful materials transition to implementation (e.g. structure, properties, performance, durability, economics, manufacturability, environmental impacts, health impacts, etc.). This capability is critical to achieve self-driving laboratories and HTE.
    Materials and processes databases (Leader / Collaborator)
Curated, national collaborative databases of materials and properties with the information and data obtained from MAPs will be established as the main repository for MAPs-acquired data and information, and to provide critical access to data for AI/ML applications. NRC-M will develop mechanisms to augment MAP-generated data by integrating other experimental and computational data sources from NRC, partners and publicly available sources.
Ultimately, with the help of our collaborators and partners, this is where we want to get to in the long term. Our goal is not to have our very own MAPs, but use this facility to support collaborate MAP opportunities.

## Slide 31
Example Detailed Work Flow: CoMnFeOx (Co:Mn:Fe = 1)
*premade 500 mM concentrations liquid
* 0.5 mM total metal concentration
From slide deck

## Slide 32
Example Detailed Work Flow: CoMnFeOx (Co:Mn:Fe = 1)
Stock solution, will never change

## Slide 33
Cell Design
Based on the redox.me bottom-loaded cell, this type of cell may offer more flexibility while also being able to more easily incorporate robotics/automation compared to previous cell design
- Reconstructed to fit a smaller design space, less electrolyte volume
Pros
+ Easier loading/unloading of working electrode
+ Easier to incorporate dual compartment for future designs
+ All probes loaded “on-board” the automated head
Cons
Electrolyte removal + washing – manageable, but will have to have methods of loading/unloading electrolyte and washing
contents after each measurement
Double o-ring system
allows for electrical
contact to the WE
while also sealing the
liquid
Station will function with an actuator to lift the contents
on and off the working electrode

## Slide 34
Washing the cell stations
Purpose is to wash prior to each new trial run, as new electrolyte will be used for each run
1. Bath Wash
Fill separate vial with water and place onto lid set-up
Will require subsequent washing steps, likely some solvent change, possibly
some motion (rotation?) to help “stir” solution?
A simple dip may be sufficient enough…checking experimentally
2. Spray Wash
Use a nozzle to lightly spray the electrolyte off of the 3 electrodes
Should be gentle “running” over the electrodes
Can build into the lid?
Spray nozzle
on side?
Spray nozzle
built into lid?

## Slide 35
Cell Electrolyte Filling
Robot arm pipettes electrolyte through the top
Problem – How to remove?
2. Small tube to add/remove liquid
3. Something on the bottom/sides?
Electrolyte will have to be added and removed for:
New salt concentrations for the electrodeposition
*maybe* to remove the wash liquid, dependent on the washing procedure
When the actuator removes the base from the lid and the glass slide is to be removed